## Slide 1
Infiltrated Double Perovskite Electrodes for Proton Conducting Steam Electrolysers
Einar Vøllestad1, Ragnar Strandbakke1, Marie-Laure Fontaine2 and Truls Norby1
1: University of Oslo, Department of Chemistry
2: SINTEF Materials and Chemistry

## Slide 2
High temperature electrolyser with novel proton ceramic tubular modules (2014-2017)
50 µm
20 µm
Fabrication of BZY-based segmented-in-series tubular electrolyser cells
Development of mixed proton-electron conducting anodes
100 µm
O2-
4H+
2H2O
3/2O2
CO2
CO+2H2
DME/Ethanol production from steam, CO2 and electricity
H2 production from steam and electricity
U
4H+
2H2
O2
2H2O
4e-
Multi-tube module development

## Slide 3: Solid state reactive sintering for BZCY based cell production
Pastes and suspensions using BaSO4, CeO2, Y2O3, ZrO2
Extrusion of fuel electrode
Electrolyte deposition
Co-sintering
SONATE 100 m2 clean room
40-ton extruder with automatic capping, cutting and air transport belt
Wet milling of SSRS based precursors
Dip-coating suspensions
Automatic dip-coater
Max 1m long tube
10-25 cm long tubes
NiO based paste
Drying in air
Drying in air

## Slide 4
Half-cells
Sintering @
1550C – 24h
100 microns
40 microns
BZCY72-NiO green tube before and after dip-coating in water based suspension
BZCY (2% Ce; 10% Y) // BZCY72-NiO
Dense electrolyte @ 1550C – 24 h
1610C – 6 h
100 microns
40 microns
BZCY72 // BZCY72-NiO

## Slide 5: Development of O2-H2O electrode, current collector and interconnect materials
100 µm

## Slide 6: Multi-tube module
Design and build module for multi-tubular testing
  7-10 tubes pr module
  Replaceable individual tubes
  Monitoring of individual tubes
Balance of Plant modelling
  Heat, flow, mass and charge balances
Goal: Test unit for 1kW electrochemical energy conversion

## Slide 7: Techno-economic evaluation of PCEC integrated with renewable energy sources
DME/Ethanol production from steam, CO2 and electricity
H2 production from steam and electricity

## Slide 8: Key differences between SOEC and PCEC - advantages and challenges
Solid Oxide Electrolyser Cell
  Well proven technology
    Scalable production
    High current densities at thermo-neutral voltage
  Long term stability challenges
    Delamination of O2-electrode
    Oxidation of H2-electrode at OCV
  High temperatures
Proton Ceramic Electrolyser Cell
  Less mature technology
    Fabrication and processing challenges
  Produces dry, pressurized H2 directly
  Potentially intermediate temperatures
    Slower degradation
    Slow O2-electrode kinetics
U
2O2-
2H2O
2H2
O2
SOEC
600-800°C
4e-
U
4H+
2H2
O2
2H2O
PCEC
400-700°C
4e-

## Slide 9: O2-electrodes for PCECs involve multiple species
Ideal
PCEC anode
O2
4H+
4e-
2H2O
4H+
Ideal H+ conductor
Typical
PCEC anode
Typical H+ conductor
2H2O
4H+
O2
4e-
2O2-
2O2-
O2
4e-
e-
e-

## Slide 10: Double Perovskite oxides show promise as O2-electrodes for PCEC
O2-
H+
BGLC: Ba1-xGd0.8La0.2+xCo2O6-δ
2H2O
4H+
O2
4e-
2O2-
2O2-
O2
4e-
100 µm
BaZr0.7Ce0.2Y0.1O3-d
BGLC
* R. Strandbakke et al., Solid State Ionics (2015)
400°C
10 Ωcm2

## Slide 11: Carefully modelled data reveal a lower active surface area for H+ than for O2-
Improved microstructure for proton reaction needed to further improve the electrode performance
50 kJmol-1
R. Strandbakke et al., Solid State Ionics (2015)
Session K5.01; 1.30 pm

## Slide 12: Infiltrated backbones may increase active surface area for PCEC O2 electrodes
Ding et al., Energy. Environ. Sci., 2014

## Slide 13: Three types of BZCY backbone microstructures were investigated
Sample name | BB1 a-d | BB2 | BB3
Powder batch | BZCY72, Cerpotech | BZCY27, Cerpotech + 1wt% ZnO | BZCY27, Cerpotech
Pore Former | Charcoal | Graphite | Charcoal
Sintering parameters | 1500°C, 5h | 1400°C, 8h | 1500°C, 5h
Deposition method | Spray coating | Brush painting | Spray Coating
BB1 a-d
BB2
BB3
50 µm
50 µm
50 µm

## Slide 14: Infiltrated BGLC yields well-dispersed nanostructure after calcination at 800°C
Cation nitrate solution: Gd(NO3)3, La(NO3)3, Co(NO3)3 and BaCO3
  Selective complexing agents:
    Ammonium EDTA (large cations), 1:1 molar ratio
    Triethanolamine (TEA) (for small Co), 2:1 molar ratio
  Wetting agent: Triton X
  Concentration: 0.5M
  Loading: 1 mL/cm2
Calcination at 800°C for 5h
5 µm

## Slide 15: Polarization resistances of infiltrated and single phase electrodes
Slight variations between the different backbone microstructures
500°C, pO2 = 1
BB1
BB2
BB3

## Slide 16: Polarization resistances of infiltrated and single phase electrodes
Slight variations between the different backbone microstructures
No observed improvement on the polarization resistance by infiltraton
500°C, pO2 = 1

## Slide 17: No apparent improvement in the active surface area of the infiltrated electrodes
Apparent increase in activation energy for proton reaction
  50 vs 70 kJmol-1
Non-significant change in pre-exponential
  Why?
log(Rp,ct,app(Ωcm2))
log(pO2(atm))
1000/T(K-1)
Ea,H≈70 kJmol-1
(modelled)

## Slide 18: Infiltrated electrodes display higher ohmic resistivity - Possible indication of current collection losses
Lower apparent electrolyte conductivity for the infiltrated samples
Insufficient electronic conductivity within the composite electrode may reduced the active surface area to the upper layers
Possible optimization strategies
  Increase BGLC loading
  Integrate current collector
  Improve microstructure
“Ohmic” resistivity:
Rbackbone
500°C, pO2 = 1
Rs

## Slide 19: Electroless deposition of Ag into BZCY backbones on BZCY tube segments
Uniform 60 nm thick silver film
1. Degrease 5 min ultrasonic bath
2. 30 sec deionized water rinse
3. 1.5 min SnCl2 surface activation
4. 30 sec rinse
5. 1.5 min PdCl2 catalyst
6. 30 sec rinse
7. Autocatalytic Ag-plating (varying time)
8. 30 sec rinse
Procedure
4 µm
4 µm

## Slide 20: Two different backbone samples deposited on tube segments studied by EIS in wet 5% H2
Backbone from calcined BZCY powder
Backbone from SSRS suspension
10 µm
50 µm
40 µm
4 µm

## Slide 21: Significant Ag-coarsening above 600°C
50 µm
50 µm
Increasing temperature
Decreasing temperature
After reduction @485°C:
After EIS measurements:

## Slide 22: SSRS based backbone presents much lower polarization resistance upon cooling

## Slide 23: Less significant silver coarsening with the SSRS backbone
Backbone from calcined BZCY powder
Backbone from SSRS suspension

## Slide 24: Conclusions
ELECTRA project aims to produce tubular PCECs for hydrogen and DME production from renewable energy sources
Development of mixed proton electron conducting electrodes is vital for efficient operation at intermediate temperatures
The double perovskite BGLC is identified as very promising material with remarkably low polarization resistance at low temperature
  Proton reaction identified as the dominating mechanism at low temperatures
Proper characterization of activation energies and pre-exponentials is essential to understand the mechanisms and identify routes for improvement
Initial results on electroless deposition of Ag into BZCY backbones shows promise
  Long term stability towards coarsening remains to be studied

## Slide 25: Acknowledgements
The research leading to these results has received funding from the European Union's Seventh Framework Programme (FP7/2007-2013) for the Fuel Cells and Hydrogen Joint Technology Initiative under grant agreement n° 621244.
My colleagues at UiO/ELECTRA:
Ragnar Strandbakke
Truls Norby
Marie-Laure Fontaine
Jose Serra
Cecilia Solis
Runar Dahl-Hansen
Nuria Bausá
Thank you for your attention!

## Slide 26: Conclusions
ELECTRA project aims to produce tubular PCECs for hydrogen and DME production from renewable energy sources
Development of mixed proton electron conducting electrodes is vital for efficient operation at intermediate temperatures
The double perovskite BGLC is identified as very promising material with remarkably low polarization resistance at low temperature
  Proton reaction identified as the dominating mechanism at low temperatures
Proper characterization of activation energies and pre-exponentials is essential to understand the mechanisms and identify routes for improvement
Initial results on electroless deposition of Ag into BZCY backbones shows promise
  Long term stability towards coarsening remains to be studied