## Slide 1
Infiltrated Double Perovskite Electrodes for Proton Conducting Steam Electrolysers
Einar Vøllestad, Ragnar Strandbakke and Truls Norby
U
4H+
2H2
O2
2H2O
PCEC
600°C
4e-

## Slide 2: Proton conducting oxides
Zr0.9Y0.1O1.95
BaZr0.9Y0.1O2.95
+ BaO 

## Slide 3: Proton conducting oxides
BaZr0.9Y0.1O2.95
From K.-D. Kreuer, 2008
Zr0.9Y0.1O1.95
+ BaO 
Kreuer, 2001

## Slide 4: Key differences between SOEC and PCEC - advantages and challenges
Solid Oxide Electrolyser Cell
  Well established technology
  Delamination of anode
  Oxidation of cathode at OCV
  High temperatures
Proton Ceramic Electrolyser Cell
  Less mature technology
  Produces dry H2 directly
  Potentially intermediate temperatures
    Slow anode kinetics
U
2O2-
2H2O
2H2
O2
SOEC
600-800°C
4e-
U
4H+
2H2
O2
2H2O
PCEC
400-700°C
4e-

## Slide 5: O2-electrodes for PCECs involve multiple species
Ideal
PCEC anode
O2
4H+
4e-
2H2O
4H+
Ideal H+ conductor
Typical
PCEC anode
Typical oxide H+ conductor
2H2O
4H+
O2
4e-
2O2-
2O2-
O2
4e-
e-
e-

## Slide 6: Double Perovskite oxides show promise as O2-electrodes for PCEC
O2-
H+
BGLC: Ba1-xGd0.8La0.2+xCo2O6-δ
2H2O
4H+
O2
4e-
2O2-
2O2-
O2
4e-
100 µm
BaZr0.7Ce0.2Y0.1O3-d
BGLC

## Slide 7: Carefully modelled data reveal a lower active surface area for H+ than for O2-
Improved microstructure for proton reaction needed to further improve the electrode performance
ln(1/RvT(Scm-1K))
log(pO2(atm))
1000/T(K-1)

## Slide 8: Infiltrated backbones may increase active surface area for PCEC O2 electrodes
Ding et al., Energy. Environ. Sci., 2014

## Slide 9: Three types of BZCY backbone microstructures were investigated
Sample name | BB1 a-d | BB2 | BB3
Powder batch | BZCY72, Cerpotech | BZCY27, Cerpotech + 1wt% ZnO | BZCY27, Cerpotech
Pore Former | Charcoal | Graphite | Charcoal
Sintering parameters | 1500°C, 5h | 1400°C, 8h | 1500°C, 5h
Deposition method | Spray coating | Brush painting | Spray Coating
BB1 a-d
BB2
BB3

## Slide 10: Infiltrated BGLC yields well-dispersed nanostructure after calcination at 800°C
Cation nitrate solution: Gd(NO3)3, La(NO3)3, Co(NO3)3 and BaCO3
  Selective complexing agents:
    Ammonium EDTA (large cations), 1:1 molar ratio
    Triethanolamine (TEA) (for small Co), 2:1 molar ratio
  Wetting agent: Triton X
  Concentration: 0.5M
  Loading: 1 mL/cm2
Calcination at 850°C for 5h

## Slide 11: Polarization resistances of infiltrated and single phase electrodes
The infiltrated electrodes display similar ASR as the single phase electrode.
Only small variations between the different backbone microstructures.
No significant increase of the active surface area

## Slide 12: Infiltrated electrodes display higher ohmic resistivity - Possible indication of current collection losses
Insufficient electronic conductivity within the composite electrode may reduced the active surface area to the upper layers
Possible optimization strategies
  Increase BGLC loading
  Integrate current collector
  Improve microstructure
Ohmic resistivity:

## Slide 13: Conclusions
Mixed proton electron conductivity is desired for PCEC electrodes
BGLC identified as a candidate material with fast electrode kinetics
  Low activation energy indicates proton reaction dominates at low temperatures
  Increased mixed proton-electron conduction is needed to utilize more of the electrode surface and further enhance the pre-exponential
Further work on improved microstructure and optimized current collection within the composite electrode is needed to further reduce the polarization resistance

## Slide 14: Acknowledgement
The research leading to these results has received funding from the European Union's Seventh Framework Programme (FP7/2007-2013) for the Fuel Cells and Hydrogen Joint Technology Initiative under grant agreement n° 621244.
My colleagues at UiO/ELECTRA:
Ragnar Strandbakke
Truls Norby
Jose Serra
Cecilia Solis
Marie-Laure Fontaine
Nuria Martínez
Thank you for your attention!

## Slide 15: Conclusions
Mixed proton electron conductivity is desired for PCEC electrodes
BGLC identified as a candidate material with fast electrode kinetics
  Low activation energy indicates proton reaction dominates at low temperatures
  Increased mixed proton-electron conduction is needed to utilize more of the electrode surface and further enhance the pre-exponential
Further work on improved microstructure and optimized current collection within the composite electrode is needed to further reduce the polarization resistance